CERTIFICATE

Certified that the work presented in the thesis entitled “Structural Health Monitoring and Retrofitting of RCC Rectangular Slabs” which is being submitted by Ms. Harpreet Gaba (Registration No. 01.28.09 Dated- 10.11.09) in fulfillment of the requirement for the award of the degree of “Doctor of Philosophy” in Civil Engineering submitted to Punjab Technical University, Jalandhar is an authentic record of candidate’s own work carried out during a period from May 2009 to December 2013 in this University under our supervision. The matter presented in this thesis has not been submitted for the award of any other degree in any University.

Supervisors

| Dr. Hardeep Singh Rai | Dr. S.P. Singh | Dr. Harvinder Singh |
| --- | --- | --- |
| Professor | Professor | Associate Professor |
| Civil Engg. Deptt. | Civil Engg. Deptt. | Civil Engg. Deptt. |
| G.N.D.Engg. College | Dr. B.R. Ambedkar National | G.N.D. Engg. College |
| Gill Road | Institute of Technology | Gill Road |
| Ludhiana-141006 | Jalandhar-14401 1 | Ludhiana-141006 |

Dedicated

to

my Parents

ACKNOWLEDGEMENT

Right at the outset, I deem to dedicate this humble venture of mine to the Almighty, the one and the only one, omnipotent, omnipresent, master of this whole universe that was always there to lead me along, holding me by the finger. Wherever I faltered along the way, He was always there to light me up in His lap, like an endearing parent to tide over obstacles.

Research in any field, aim not only at finding new facts but also confirm the validity of the already known facts. This study might me first like a small drop in the vast ocean of research but it is drops like these that make up the ocean. To survive, the human race has to keep making headway and all genuine progress results from finding new facts.

Endeavor, no matter how spirited and consistent does little to steer one, unless coupled with discrete guidance. With great pleasure I take this opportunity to thank all those who helped me in the successful completion of my work.

Not to fulfill a formality, but to express the feeling in my heart, I gratefully acknowledge the keen personnel interest and guidance rendered by my esteemed teacher, mentor and Supervisor Dr. Hardeep Singh Rai, Professor, Department of Civil Engineering, Guru Nanak Dev Engineering College, Ludhiana for his keen personal interest, whole hearted support and encouragement. It was his constant guidance, vast knowledge, exceptional perfection, advice and counseling that I was able to complete this seemingly difficult task. I shall invariably regard him as an inexhaustible source of inspiration forever.

I acknowledge and sincerely appreciate the contribution of my Co-supervisor Dr. S.P. Singh, Professor, Department of Civil Engineering, Dr. B.R. Ambedkar National Institute of Technology, Jalandhar under whose tutelage this study was conducted. His adroit altruism and graceful guidance helped me winnow the ocean of data and wield the facts. I shall always remain indebted to him for his balanced judgment, fervent interest and accommodative attitude.

I am highly indebted to my Co-supervisor, Dr. Harvinder Singh, Associate Professor, Department of Civil Engineering, Guru Nanak Dev Engineering College, Ludhiana for his keen personal interest, whole hearted support and encouragement. His vast experience and immense knowledge always bailed me out, whenever I got stuck during the course of thi s study.

I am thankful to Tata Tiscon Ltd. and H.S. Traders for their cooperation and timely supply of the material that helped in the successful completion of my work

My special thanks to my parents and other family members for their affection, unstinted support and for their blessings, love, care, constant encouragement and support rendered during my course of study.

I thankfully acknowledge the indigenous suggestions, sincere advice and constructive criticism of the teaching and non-teaching staff of Department of Civil Engineering, Guru Nanak Dev Engineering College, Ludhiana for their kind support and constant motivation.

Above all, I thank Almighty for everything.

(Harpreet Gaba)

LIST OF TABLES

| Table No. | Title | Page No. |
| --- | --- | --- |
| 2.1 | Proposed Damage Index for Different States of Damage | 38 |
| 3.1 | Physical properties of Ordinary Portland Cement | 41 |
| 3.2 | Properties of Fine Aggregates | 42 |
| 3.3 | Specifications of Slab | 44 |
| 3.4 | Properties of GFRP Sheets | 45 |
| 3.5 | Properties of wire mesh for Ferrocement | 46 |
| 3.6 | Properties of MS Sheet | 46 |
| 3.7 | Properties of Primer | 47 |
| 3.8 | Properties of Epoxy | 48 |
| 4.1 | Material Properties of Concrete | 65 |
| 4.2 | Material Properties of Reinforcement | 67 |
| 5.1 | Rebound Hammer and Ultrasonic Pulse Velocity values at marked points of virgin slabs S11 | 83 |
| 5.2 | Rebound Hammer and Ultrasonic Pulse Velocity values at marked points of virgin slabs S12 | 84 |
| 5.3 | Rebound Hammer and Ultrasonic Pulse Velocity values at marked points of virgin slabs S13 | 85 |
| 5.4 | Rebound Hammer and Ultrasonic Pulse Velocity values at marked points of virgin slabs S21 | 86 |
| 5.5 | Rebound Hammer and Ultrasonic Pulse Velocity values at marked points of virgin slabs S22 | 87 |
| 5.6 | Rebound Hammer and Ultrasonic Pulse Velocity values at marked points of virgin slabs S23 | 88 |
| 5.7 | Rebound Hammer Number and Ultrasonic Pulse Velocity values after loading test at marked points of virgin slabs S11 | 93 |
| 5.8 | Rebound Hammer and Ultrasonic Pulse Velocity values after loading test at marked points of slab S12 | 94 |
| 5.9 | Rebound Hammer and Ultrasonic Pulse Velocity values after loading test at marked points of slab S13 | 95 |
| 5.10 | Rebound Hammer and Ultrasonic Pulse Velocity values after loading test at marked points of slab S21 | 96 |
| 5.11 | Rebound Hammer and Ultrasonic Pulse Velocity values at marked points of slab S22 | 97 |
| 5.12 | Rebound Hammer and Ultrasonic Pulse Velocity values at marked points of slab S23 | 98 |
| 5.13 | Value of Load (A, B, C and D) at various stages of Crack Development | 113 |

LIST OF FIGURES

| Fig. No. | Title | Page No. |
| --- | --- | --- |
| 3.1 | Outline of the Test Programme | 40 |
| 3.2 | M-Brace Epoxy consist of Base and Hardener | 47 |
| 3.3 | UPV test for (a) semi-direct, (b) indirect and (c) direct test | 49 |
| 3.4 | Ultrasonic Pulse Velocity Testing Machine | 49 |
| 3.5 | Rebound Hammer | 50 |
| 3.6 | Reinforcement of Slabs | 51 |
| 3.7 | Curing of slabs | 51 |
| 3.8 | Slab being taken inside the Laboratory | 53 |
| 3.9 | Reaction Frame of Heavy Testing Laboratory | 53 |
| 3.10 | Steel balls used for load conversion | 54 |
| 3.11 | Work in Progression | 54 |
| 3.12 | Points Marked for NDT | 55 |
| 3.13 | Rebound Hammer Test | 56 |
| 3.14 | Application of Epoxy | 58 |
| 3.15 | Placing of GFRP | 59 |
| 3.16 | Rolling of GFRP | 59 |
| 3.17 | Placing of MS Sheet | 60 |
| 3.18 | Retrofitting with Ferrocement | 60 |
| 4.1 | Concrete Stress-Strain Curve in Compression (CEB-FIP Model Code 1990). | 66 |
| 4.2 | Bilinear Stress–Strain Law for Reinforcement. | 68 |
| 4.3 | Data tree for Run | 70 |
| 4.4 | Parameters for Solutions | 70 |
| 4.5 | Model of slab S1 | 73 |
| 4.6 | Reinforcement in slab S1 | 73 |
| 4.7 | Meshed form of Reinforcement in slab S1 | 74 |
| 4.8 | Solid model of slab S1 | 75 |
| 4.9 | Meshed model of Slab S1 | 75 |
| 4.10 | Meshed Model of GFRP retrofitted Slab S11 | 76 |
| 4.11 | Meshed Model of GFRP retrofitted Slab S11 | 76 |
| 4.12 | Meshed Model of Ferrocement retrofitted Slab S12 | 77 |
| 4.13 | Meshed Model of MS plate retrofitted Slab S13 | 77 |
| 4.14 | Solid Model of slab S2 | 78 |
| 4.15 | Reinforced Model of Slab S2 | 78 |
| 4.16 | Meshed model of Slab S2 | 79 |
| 4.17 | Meshed Model of GFRP retrofitted Slab S21 | 79 |
| 4.18 | Meshed Model of Ferrocement retrofitted Slab S22 | 80 |
| 4.19 | Meshed Model of MS plate retrofitted Slab S23. | 80 |
| 5.1 | Initiation of cracks in slabs (typical) | 89 |
| 5.2 | Cracks in slabs (typical) | 90 |
| 5.3 | Development of cracks (typical) | 90 |
| 5.4 | Propagation of cracks (typical) | 91 |
| 5.5 | Load-Deflection curve of slab S11 (before and after GFRP retrofitting) | 100 |
| 5.6 | Load-Deflection curve of slab S2 1 (before and after GFRP retrofitting) | 100 |
| 5.7 | Load-Deflection curve of slab S12 (before and after ferrocement retrofitting) | 101 |
| 5.8 | Load-Deflection curve of slab S22 (before and after retrofitting with ferrocement) | 101 |
| 5.9 | Load-Deflection curve of slab S13 (before and after MS Plate retrofitting) | 102 |
| 5.10 | Load-Deflection curve of slab S23 (before and after MS Plate retrofitting) | 102 |
| 5.11 | Load-Deflection curve of S1 slabs retrofitted with different Materials | 103 |
| 5.12 | Load-Deflection curve of S2 slabs retrofitted with different Materials | 103 |
| 5.13 | Analytical and Experimental Load-Deflection values of virgin slabs S1 | 104 |
| 5.14 | Analytical and Experimental Load-Deflection values of virgin slabs S2 | 105 |
| 5.15 | Analytical and Experimental Load-Deflection values of retrofit slab S11 | 105 |
| 5.16 | Analytical and Experimental Load-Deflection values of GFRP retrofit slab S21 | 106 |
| 5.17 | Analytical and Experimental Load-Deflection values of Ferrocement retrofit Slab S12 | 106 |
| 5.18 | Analytical and Experimental Load-Deflection values of Ferrocement retrofit slab S22 | 107 |
| 5.19 | Analytical and Experimental Load-Deflection values of MS Plate retrofit slab S13 | 107 |
| 5.20 | Analytical and Experimental Load-Deflection values of MS Plate retrofit slab S23 | 108 |
| 5.21 | Analytical Load-Deflection curve of S1 slab retrofitted with different materials | 108 |
| 5.22 | Analytical Load-Deflection curve of S2 slab retrofitted with different materials | 109 |
| 5.23 | Debonding of GFRP in Slab (typical). | 109 |
| 5.24 | Debonding of GFRP at Corners (typical). | 110 |
| 5.25 | GFRP failure pattern followed similar trend on other side of the slab (typical) | 110 |
| 5.26 | Failure pattern of slab retrofitted with Ferrocement (typical) | 111 |
| 5.27 | Debonding of MS Plate (typical) | 111 |
| 5.28 | Debonding of MS Plate at Corners (typical) | 112 |
| 5.29 | Complete Split-up of MS Plate (typical) | 112 |
| 5.30 | Generalised crack pattern at various stages of loading | 113 |
| 5.31 | Relation between damage index and ratio of areas for GFRP retrofitted slab | 116 |
| 5.32 | Relation between Damage Index and (σm k h) for ferrocement for different values of d1/d | 116 |
| 5.33 | Relation between Damage Index and Thickness (t) of Mild Steel Plate. | 117 |

LIST OF ABBREVIATIONS

	Diameter of wire mesh

ck	Characteristic strength of concrete

fe	Effective strain in GFRP

m	Tensile strength of cement mortar

Af	Cross-section area of FRP

Ast	Area of tensile reinforcement per meter run

b	Width of the slab

CFRP	Carbon Fiber Reinforced Polymer

Cu	Compressive force of concrete

d	Depth of slab from top up to centre of reinforcement

d1	Depth of retrofitted slab from top up to centre of retrofitted material

Ef	Modulus of elasticity of FRP

fy	Grade of steel

GFRP	Glass Fiber Reinforced Polymer

h	Thickness of ferrocement layer

I	Moment of Inertia

k	constant = SF 

n	No. of bars per meter width

NDT	Non Destructive Testing

RC	Reinforced Concrete

s	Specific surface area

SF	         	Specific surface factor

SHM         	Structural Health Monitoring

Tm         	Tensile force of retrofitted material

Ts         	Tensile force of reinforced bars Ultrasonic Pulse Velocity

UPV         	Ultrasonic Pulse Velocity

xu         	Depth of neutral axis from top

Z		Section modulus

єcu         	Strain in concrete

єm         	Strain in retrofitted material at the bottom

єst        	Strain in reinforcement

CONTENTS

| CHAPTER | TITLE |  |  | PAGE NO. |
| --- | --- | --- | --- | --- |
|  | Certificate |  |  | i |
|  | Dedication |  |  | ii |
|  | Acknowledgement |  |  | iii |
|  | List of Tables |  |  | v |
|  | List of Figures |  |  | vii |
|  | List of Abbreviations |  |  | xi |
| 1. | INTRODUCTION |  |  | 1-5 |
|  | 1.1 | General |  | 1 |
|  | 1.2 | Problem Formulation |  | 2 |
|  |  | 1.2.1 | Need and Significance of Present Research Work | 2 |
|  |  | 1.2.2 | Programme /Technical Work / Methodology / Equipment Required / Laboratory Work Facility | 3 |
|  |  | 1.2.3 | Objectives of the Present Investigation | 3 |
|  |  | 1.2.4 | Scope of Study | 4 |
|  |  | 1.2.5 | Methodology | 4 |
|  | 1.3 | Organization of the Thesis |  | 5 |
| 2. | LITERATURE REVIEW |  |  | 6-39 |
|  | 2.1 | General |  | 6 |
|  | 2.2 | Literature Review |  | 6 |
|  |  | 2.2.1 | Strengthening of Structural Elements | 6 |
|  |  | 2.2.2 | Health Monitoring of Structures | 21 |
|  |  | 2.2.3 | Finite Element Modeling | 28 |
|  | 2.3 | Damage Index |  | 38 |
|  | 2.4 | Comments on the Present State of Art |  | 38 |
|  | 2.5 | Research Significance |  | 39 |
|  | 2.6 | Closure |  | 39 |
| 3. | EXPERIMENTAL PROGRAMME |  |  | 40-61 |
|  | 3.1 | General |  | 40 |
|  | 3.2 | Test Programme |  | 40 |
|  | 3.3 | Materials Characterization |  | 41 |
|  |  | 3.3.1 | Cement | 41 |
|  |  | 3.3.2 | Fine Aggregates | 41 |
|  |  | 3.3.3 | Coarse Aggregates | 42 |
|  |  | 3.3.4 | Concrete Mix | 42 |
|  |  | 3.3.5 | Water | 42 |
|  |  | 3.3.6 | Steel | 43 |
|  |  | 3.3.7 | Section of Slab | 43 |
|  |  | 3.3.8 | Retrofitting Materials | 44 |
|  |  | 3.3.9 | Bonding materials | 46 |
|  | 3.4 | Major Equipments Used |  | 48 |
|  |  | 3.4.1 | Reaction Frame | 48 |
|  |  | 3.4.2 | Ultrasonic Pulse Velocity Equipment | 48 |
|  |  | 3.4.3 | Rebound Hammer Testing Equipment | 49 |
|  | 3.5 | Experimental Programme |  | 50 |
|  |  | 3.5.1 | Casting of Slabs | 50 |
|  |  | 3.5.2 | Testing Methodology | 52 |
|  | 3.6 | Steps for preparing surface for retrofitting |  | 57 |
|  | 3.7 | Closure |  | 61 |
| 4. | FINITE ELEMENT MODELING |  |  | 62-81 |
|  | 4.1 | General |  | 62 |
|  | 4.2 | Prominence of Finite Element Modeling |  | 62 |
|  | 4.3 | Modeling Methodology |  | 63 |
|  | 4.4 | Terminology in ATENA 3D |  | 63 |
|  | 4.5 | Steps in Finite Element Modeling |  | 64 |
|  |  | 4.5.1 | Coordinates | 64 |
|  |  | 4.5.2 | Material from Direct Definition | 64 |
|  |  | 4.5.3 | Modeling the slab | 68 |
|  |  | 4.5.4 | Modeling the reinforcement | 69 |
|  |  | 4.5.5 | Macroelements | 69 |
|  |  | 4.5.6 | Load Cases | 69 |
|  |  | 4.5.7 | Run Analysis | 70 |
|  |  | 4.5.8 | Run | 72 |
|  |  | 4.5.9 | Post Processing | 72 |
|  | 4.6 | Finite Element Modeling of Slabs |  | 72 |
|  | 4.7 | Closure |  | 81 |
| 5. | ANALYSIS OF RESULTS AND DISCUSSION |  |  | 82-118 |
|  | 5.1 | General |  | 81 |
|  | 5.2 | Non Destructive Testing on Slabs Before Loading |  | 82 |
|  | 5.3 | Loading Test Results Before Retrofitting |  | 89 |
|  | 5.4 | Non Destructive Test Results After Loading Test |  | 92 |
|  | 5.5 | Loading Test Results After Retrofitting |  | 99 |
|  | 5.6 | Finite Element Modelling Results |  | 104 |
|  | 5.7 | Post Cracking Behavior of Retrofitted Slabs |  | 109 |
|  | 5.8 | Discussion |  | 113 |
|  | 5.9 | Closure |  | 117 |
|  | 5.10 | Contributions of Present Investigation |  | 118 |
| 6. | CONCLUSION |  |  | 119-129 |
|  | 6.1 | General |  | 119 |
|  | 6.2 | Conclusions |  | 119 |
|  | 6.3 | Scope For Future Work |  | 121 |
|  |  | Research Publications |  | 122 |
|  | REFERENCES |  |  | 123-131 |
|  | ANNEXURES |  |  | I-XIII |